|  | EN 10204 TYPE 2.1 Declaration of Compliance QUALITY CONTROLLED DOCUMENT |
| --- | --- |

| Certificate No: | AM-2026-00847 | Date: | 22 February 2026 |
| --- | --- | --- | --- |
| Order No: | PO-2026-1542 | Delivery Note: | DN-2026-0847 |
| Customer: | Nordic Offshore Solutions AS | Heat No: | H847263 |
| Customer Address: | Havnegata 15, 5003 Bergen, Norway | Batch No: | B2026-0142 |

MANUFACTURER DETAILS

| Aurelian Manufacturing AS Industriveien 42 4033 Stavanger Norway | Tel: +47 51 84 32 00 Email: quality@aurelian-mfg.no Web: www.aurelian-mfg.no VAT: NO 987 654 321 MVA |
| --- | --- |

MATERIAL DESCRIPTION

| Material Grade: | Stainless Steel 316L | Standard: | EN 10216-5 / ASTM A312 |
| --- | --- | --- | --- |
| Product: | Seamless Stainless Steel Pipes | Quantity: | 48 pcs |
| Surface Finish: | 2B / Pickled | Total Weight: | 2,450 kg |

PRODUCT SPECIFICATIONS

| Item | Size / Dimensions | Length | Quantity | Weight |
| --- | --- | --- | --- | --- |
| 1 | DN 50 (60.3 x 2.77 mm) | 6.0 m | 12 | 510 kg |
| 2 | DN 80 (88.9 x 3.05 mm) | 6.0 m | 18 | 980 kg |
| 3 | DN 100 (114.3 x 3.05 mm) | 6.0 m | 18 | 960 kg |

CHEMICAL COMPOSITION (% by mass)

| Element | C | Si | Mn | P | S | Cr | Ni | Mo | N |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Specification | ≤ 0.030 | ≤ 1.00 | ≤ 2.00 | ≤ 0.045 | ≤ 0.030 | 16.0-18.0 | 10.0-14.0 | 2.0-3.0 | ≤ 0.10 |
| Actual | 0.018 | 0.42 | 1.38 | 0.028 | 0.001 | 16.85 | 10.52 | 2.14 | 0.045 |

MECHANICAL PROPERTIES

| Property | Specification | Test Result |
| --- | --- | --- |
| Tensile Strength (Rm) | ≥ 485 MPa | 572 MPa |
| Yield Strength (Rp0.2) | ≥ 170 MPa | 298 MPa |
| Elongation (A) | ≥ 35% | 52% |
| Hardness (HB) | ≤ 217 HB | 168 HB |

COMPLIANCE STATEMENT

This Declaration of Compliance (EN 10204 Type 2.1) confirms that the products supplied conform to the requirements of the order, without inclusion of test results.

The manufacturer declares that the supplied materials are in accordance with the specifications stated in the purchase order and applicable standards.

AUTHORIZED SIGNATURE

| Name: Erik Hansen | Date: 22 February 2026 |
| --- | --- |
| Title: Quality Manager | Department: Quality Assurance |

This declaration is issued under the responsibility of the manufacturer.

Aurelian Manufacturing AS | EN 10204 Type 2.1 Certificate | Ref: AM-2026-00847
This document is electronically generated and valid without signature when accompanied by a valid digital seal.