|  | EN 10204 TYPE 2.2 Test Report QUALITY CONTROLLED DOCUMENT |
| --- | --- |

| Certificate No: | AM-2026-00847 | Date: | 22 February 2026 |
| --- | --- | --- | --- |
| Order No: | PO-2026-1542 | Delivery Note: | DN-2026-0847 |
| Customer: | Nordic Offshore Solutions AS | Heat No: | H847263 |
| Customer Address: | Havnegata 15, 5003 Bergen, Norway | Batch No: | B2026-0142 |

MANUFACTURER DETAILS

| Aurelian Manufacturing AS Industriveien 42 4033 Stavanger Norway | Tel: +47 51 84 32 00 Email: quality@aurelian-mfg.no Web: www.aurelian-mfg.no VAT: NO 987 654 321 MVA |
| --- | --- |

MATERIAL DESCRIPTION

| Material Grade: | Stainless Steel 316L | Standard: | EN 10216-5 / ASTM A312 |
| --- | --- | --- | --- |
| Product: | Seamless Stainless Steel Pipes | Quantity: | 48 pcs |
| Surface Finish: | 2B / Pickled | Total Weight: | 2,450 kg |

PRODUCT SPECIFICATIONS

| Item | Size / Dimensions | Length | Quantity | Weight |
| --- | --- | --- | --- | --- |
| 1 | DN 50 (60.3 x 2.77 mm) | 6.0 m | 12 | 510 kg |
| 2 | DN 80 (88.9 x 3.05 mm) | 6.0 m | 18 | 980 kg |
| 3 | DN 100 (114.3 x 3.05 mm) | 6.0 m | 18 | 960 kg |

CHEMICAL COMPOSITION (% by mass)

| Element | C | Si | Mn | P | S | Cr | Ni | Mo | N |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Specification | ≤ 0.030 | ≤ 1.00 | ≤ 2.00 | ≤ 0.045 | ≤ 0.030 | 16.0-18.0 | 10.0-14.0 | 2.0-3.0 | ≤ 0.10 |
| Actual | 0.018 | 0.42 | 1.38 | 0.028 | 0.001 | 16.85 | 10.52 | 2.14 | 0.045 |

MECHANICAL PROPERTIES

| Property | Specification | Test Result |
| --- | --- | --- |
| Tensile Strength (Rm) | ≥ 485 MPa | 572 MPa |
| Yield Strength (Rp0.2) | ≥ 170 MPa | 298 MPa |
| Elongation (A) | ≥ 35% | 52% |
| Hardness (HB) | ≤ 217 HB | 168 HB |

COMPLIANCE STATEMENT

This Test Report (EN 10204 Type 2.2) confirms that the products supplied conform to the requirements of the order, based on non-specific inspection.

Test results are derived from non-specific inspection on products manufactured using the same production process but not necessarily from the actual products delivered.

AUTHORIZED SIGNATURE

| Quality Assurance Department |  |
| --- | --- |
| Name: Erik Hansen | Date: 22 February 2026 |
| Title: Quality Manager | Signature: _______________ |

This test report is issued based on non-specific inspection results.

Aurelian Manufacturing AS | EN 10204 Type 2.2 Certificate | Ref: AM-2026-00847
This document is electronically generated and valid without signature when accompanied by a valid digital seal.