|  | EN 10204 TYPE 3.2 Inspection Certificate 3.2 QUALITY CONTROLLED DOCUMENT |
| --- | --- |

| Certificate No: | AM-2026-00847 | Date: | 22 February 2026 |
| --- | --- | --- | --- |
| Order No: | PO-2026-1542 | Delivery Note: | DN-2026-0847 |
| Customer: | Nordic Offshore Solutions AS | Heat No: | H847263 |
| Customer Address: | Havnegata 15, 5003 Bergen, Norway | Batch No: | B2026-0142 |

MANUFACTURER DETAILS

| Aurelian Manufacturing AS Industriveien 42 4033 Stavanger Norway | Tel: +47 51 84 32 00 Email: quality@aurelian-mfg.no Web: www.aurelian-mfg.no VAT: NO 987 654 321 MVA |
| --- | --- |

MATERIAL DESCRIPTION

| Material Grade: | Stainless Steel 316L | Standard: | EN 10216-5 / ASTM A312 |
| --- | --- | --- | --- |
| Product: | Seamless Stainless Steel Pipes | Quantity: | 48 pcs |
| Surface Finish: | 2B / Pickled | Total Weight: | 2,450 kg |

PRODUCT SPECIFICATIONS

| Item | Size / Dimensions | Length | Quantity | Weight |
| --- | --- | --- | --- | --- |
| 1 | DN 50 (60.3 x 2.77 mm) | 6.0 m | 12 | 510 kg |
| 2 | DN 80 (88.9 x 3.05 mm) | 6.0 m | 18 | 980 kg |
| 3 | DN 100 (114.3 x 3.05 mm) | 6.0 m | 18 | 960 kg |

CHEMICAL COMPOSITION (% by mass)

| Element | C | Si | Mn | P | S | Cr | Ni | Mo | N |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Specification | ≤ 0.030 | ≤ 1.00 | ≤ 2.00 | ≤ 0.045 | ≤ 0.030 | 16.0-18.0 | 10.0-14.0 | 2.0-3.0 | ≤ 0.10 |
| Actual | 0.018 | 0.42 | 1.38 | 0.028 | 0.001 | 16.85 | 10.52 | 2.14 | 0.045 |

MECHANICAL PROPERTIES

| Property | Specification | Test Result |
| --- | --- | --- |
| Tensile Strength (Rm) | ≥ 485 MPa | 572 MPa |
| Yield Strength (Rp0.2) | ≥ 170 MPa | 298 MPa |
| Elongation (A) | ≥ 35% | 52% |
| Hardness (HB) | ≤ 217 HB | 168 HB |

TEST RESULTS

| Visual Inspection | Acceptable - No defects observed |
| --- | --- |
| Dimensional Inspection | Within tolerance per EN 10216-5 |
| Hydrostatic Test | Tested at 70 bar - No leakage |
| Eddy Current Test | Acceptable per EN 10246-3 |
| PMI Verification | Verified - Material composition confirmed |

COMPLIANCE STATEMENT

This Inspection Certificate (EN 10204 Type 3.2) confirms that the products supplied conform to the requirements of the order.

The test results presented are based on specific inspection and testing of the actual products delivered. Testing was witnessed and validated by both the manufacturer's authorized inspection representative and the purchaser's designated representative / authorized inspection body.

AUTHORIZED SIGNATURES

| Manufacturer's Representative | Purchaser's Representative |
| --- | --- |
| Name: Dr. Ingrid Solberg | Name: Magnus Olsen |
| Title: Chief Quality Inspector | Organization: DNV GL |
| Cert. No: QI-2024-0847 | Inspector ID: DNV-4521-NO |
| Date: 22 February 2026 | Date: 22 February 2026 |

[MANUFACTURER STAMP]                    [INSPECTION BODY STAMP]

This certificate is validated by both the manufacturer's authorized inspection representative and the purchaser's designated representative.

Aurelian Manufacturing AS | EN 10204 Type 3.2 Certificate | Ref: AM-2026-00847
This document is electronically generated and valid without signature when accompanied by a valid digital seal.